## Slide 1
BNF-CH527 vs Fine Grind

## Slide 2
Masstone and Tint
BNF-CH527
BNF-CH527 FG
DE: 1.53
Strength: 108%
BNF-CH527
BNF-CH527 FG

## Slide 3
Heat Stability
BNF-CH527
5 min, 300C Hold
DE: 16.30
DE: 8.11
BNF-CH527 Fine Grind
5 min, 300C Hold

## Slide 4
Lightfastness
Exposed
Unexposed
DE: 4.65
DE: 4.43
BNF-CH527 Fine Grind
Unexposed
BNF-CH527
Exposed

## Slide 5
ZQ-17 vs BNF-CH527 FG
ZQ-17
BNF-CH527 FG
Masstone
BNF-CH527 Fine Grind
5 min, 300C Hold
ZQ-17
5 min, 300C Hold
Heat Hold
DE: 18.19
DE: 8.11

## Slide 6
Long Plate out
40% 800g
Clean
STD BNF-CH527
BNF-CH527 FG

## Slide 7
Long Plate out
40% 800g Chips
STD BNF-CH527
Had to spoon feed.
Strands were very puffy.
BNF-CH527 FG
Had to spoon feed.
Strands were uniform.
Both took similar time to extrude and mold.